## Slide 1: Updates 2-4-21
Stanford University
2/4/21
Initial RRAM Characteristics

## Slide 2: Status
Done with FORM, SET, RESET, Target Resistance
Done with checkerboard tests
Done with bitstream programming
Speed optimizations
Some yield optimizations
Done with full array FORM
Done with full array yield analysis
In progress (running currently):
Full array programming

## Slide 3: Operation conditions
Operation | READ | FORM | SET | RESET
BL/SL Start (V) | 0.2 (BL) | 2 | 2 | 3
BL/SL Stop (V) | N/A | 4 | 2 | 3
BL/SL Step (V) | N/A | 0.5 | N/A | N/A
WL Start (V) | 2.5 | 0.9 | 0.9 | 0.9
WL Stop (V) | N/A | 1.5 | 1.5 | 1.5
WL Step (V) | N/A | 0.05 | 0.1 | 0.1
WL Pulse Width (us) | 2000 | 2000 | 10 | 10
Stop Condition | N/A | < 50kΩ | Below target (9-11kΩ) | Above target (70-90kΩ)
Loop Order | N/A | WL outer/ BL inner | WL only | WL only
Total FORM Time:
3 cells/s
=
7 hrs/array
Total Prog Time:
2 cells/s
=
8 hrs/array

## Slide 4: Notes on READ
Using 560Ω shunt resistor and reading voltage across it
Collecting 100 samples
2ms for BL voltage to ramp up to 200mV, then read current at 1MHz
Includes the transistor voltage drop

## Slide 5: FORMing Statistics and Yield
39 Failures

## Slide 6: Rerun FORM on failed cells
Important not to over-SET
Rerunning once more successfully FORMED 38/39 failed cells
After that, rerunning on the final failed cell FORMED it
Giving 100% yield!

## Slide 7: FORMing Statistics and Yield (Final)