## Slide 1: Updates 2-4-21
Stanford University
2/4/21
RRAM Programming

## Slide 2: Status
Done with FORM, SET, RESET, Target Resistance
Done with checkerboard tests
Done with bitstream programming
Speed + yield optimizations
Done with full array FORM
Done with full array yield analysis
Done with full array programming of one array (first iteration)
In progress:
    Tail distribution reprogramming
    Process more arrays with different LRS/HRS
    Finalize figures

## Slide 3: Operation conditions
Operation | READ | FORM | SET | RESET
BL/SL Start (V) | 0.2 (BL) | 2 | 2 | 3
BL/SL Stop (V) | N/A | 4 | 2 | 3
BL/SL Step (V) | N/A | 0.5 | N/A | N/A
WL Start (V) | 2.5 | 0.9 | 0.9 | 0.9
WL Stop (V) | N/A | 1.5 | 1.5 | 1.5
WL Step (V) | N/A | 0.05 | 0.1 | 0.1
WL Pulse Width (us) | 2000 | 2000 | 10 | 10
Stop Condition | N/A | < 50kΩ | Below target (9-11kΩ) | Above target (70-90kΩ)
Loop Order | N/A | WL outer/ BL inner | WL only | WL only
Total FORM Time:
3 cells/s
=
7 hrs/array
Total Prog Time:
4 cells/s
=
6 hrs/array
Switched to analog driver

## Slide 4: Full-Array FORMing Yield
Initial:
39 Failures…
Small number of FORM failures due to 1.5V VWL limit
Failures happen further down the BL/WL, probably due to IR drop
Important not to over-SET
    Cannot increase limit!
Rerunning FORM for failed cells successfully FORMed 38/39
Rerunning a second time on the final failed cell FORMed it
Result: 100% FORM yield!

## Slide 5: Full-Array FORMing Statistics
Certain BLs seem to have higher VWL and hence lower resistance

## Slide 6: Full-Array FORMing Statistics

## Slide 7: Full-Array Programming

## Slide 8: Full-Array Programming

## Slide 9: Full-Array Programming

## Slide 10: Full-Array Programming

## Slide 11: Full-Array Programming

## Slide 12: Full-Array Programming

## Slide 13: Full-Array Programming