## Slide 1: Updates 2-4-21
Stanford University
2/4/21
RRAM Programming

## Slide 2: Status
Done with FORM, SET, RESET, Target Resistance
Done with checkerboard tests
Done with bitstream programming
Speed + yield optimizations
Done with full array FORM
Done with full array yield analysis
Done with full array programming of one array
In progress:
    Process more arrays with different LRS/HRS
    Finalize figures

## Slide 3: Operation conditions
Operation | READ | FORM | SET | RESET
BL/SL Start (V) | 0.2 (BL) | 2 | 2 | 3
BL/SL Stop (V) | N/A | 4 | 2 | 3
BL/SL Step (V) | N/A | 0.5 | N/A | N/A
WL Start (V) | 2.5 | 0.9 | 0.9 | 0.9
WL Stop (V) | N/A | 1.5 | 1.5 | 1.5
WL Step (V) | N/A | 0.05 | 0.1 | 0.1
WL Pulse Width (us) | 2000 | 2000 | 10 | 10
Stop Condition | N/A | < 50kΩ | Below target (9-11kΩ) | Above target (70-90kΩ)
Loop Order | N/A | WL outer/ BL inner | WL only | WL only
Total FORM Time:
3 cells/s
=
7 hrs/array
Total Prog Time:
4 cells/s
=
6 hrs/array
Switched to analog driver

## Slide 4: Notes on READ
Using 560Ω shunt resistor and reading voltage across it
Collecting 100 samples
2ms for BL voltage to ramp up to 200mV, then read current at 1MHz
Includes the transistor voltage drop

## Slide 5: Full-Array FORMing Yield
Initial:
39 Failures…
Small number of FORM failures due to 1.5V VWL limit
Failures happen further down the BL/WL, probably due to IR drop
Important not to over-SET
    Cannot increase limit!
Rerunning FORM for failed cells successfully FORMed 38/39
Rerunning a second time on the final failed cell FORMed it
Result: 100% FORM yield!

## Slide 6: Full-Array FORMing Statistics
Certain BLs seem to have higher VWL and hence lower resistance

## Slide 7: Full-Array FORMing Statistics

## Slide 8: Cell Programming

## Slide 9: Cell Programming

## Slide 10: Iterative Improvement
Narrowing of resistance distributions